**PU Foam Waste Tree**  
**Executive Summary & Table of Contents**

**Table of Contents**

**1. Product & Design Definition Losses**  
1.1 Incorrect Foam Grade Selection  
1.2 Over-Specification of Foam Properties  
1.3 Component Shape Complexity  
1.4 Unnecessary Tolerances or Finish Requirements  
1.5 Design Misalignment with Plant Capabilities

**2. Foam Production Planning Losses**  
2.1 Batch Fragmentation  
2.2 Color Changeover Waste  
2.3 Density Changeover Waste  
2.4 Cleaning and Flush Waste  
2.5 Paper Setup Waste  
2.6 Premature Runs from Inventory Gaps  
2.7 Misaligned Planning vs Curing Constraints

**3. Chemical Reaction Losses**  
3.1 Gas Phase Loss  
3.2 Off-Ratio Chemistry  
3.3 Catalyst Drift or Deactivation  
3.4 Surfactant Incompatibility or Decay  
3.5 Moisture or Contamination-Based Failures  
3.6 Chemical Settling or Separation  
3.7 Raw Material Quality Variance

**4. Block Geometry & Rise Losses**  
4.1 Crust (Skin) Formation  
4.2 Start and Stop Block Defects  
4.3 Dome or Sinkback Profiles  
4.4 Shoulder Collapse or Footprint Effects  
4.5 Stratification or Layering  
4.6 Bottom Cavitation or Dense Skins  
4.7 Fallplate or Conveyor Instability

**5. Curing & Stabilization Losses**  
5.1 Shrinkage after Rise  
5.2 Delayed Cure or Soft Core  
5.3 Post-Rise Warping or Collapse  
5.4 Internal Thermal Cracking  
5.5 Humidity-Induced Inconsistency  
5.6 Temperature Gradient Effects in Storage

**6. Conversion Planning Losses**  
6.1 Poor Block-to-Part Matching  
6.2 Inefficient CNC Nesting Due to Shape Mix  
6.3 Component Overproduction Due to Order Fragmentation  
6.4 Misalignment of Inventory vs Shape Yield  
6.5 Short-Block Conversion Mismatch  
6.6 Multi-Grade Conversion Conflicts

**7. Cutting & Component Conversion Losses**  
7.1 Saw Kerf and Blade Width Loss  
7.2 Tolerance Buffer Loss  
7.3 CNC Overcutting or Misalignment  
7.4 Dust and Crumb Generation  
7.5 Clickability and Edge Quality Defects  
7.6 Scrap from Part Labeling or Sorting Errors

**8. Quality & Compliance Rejection Losses**  
8.1 ILD/CDH Test Failures  
8.2 Density Out-of-Spec  
8.3 Fogging, VOC, or Odor Failure  
8.4 Compression Set or Tensile Failure  
8.5 Flame Retardancy Test Rejection  
8.6 Dimensional Recovery or Shrinkage Failures

**9. Handling, Storage & Fulfillment Losses**  
9.1 Stacking Compression or Deformation  
9.2 Block Denting or Edge Damage  
9.3 Labeling or Tracking Errors  
9.4 FIFO Breakdown and Aging Inventory  
9.5 Transport Vibration or Moisture Exposure  
9.6 Customer Return Due to Handling Faults

End of Executive Summary & ToC